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Product Description

Wall & Floor Tile Grout is a specially formulated cement- based polymer modified grouting compound designed to grout tile grout joints up to a width of 8mm. Tile Tak Tile Grout incorporates additives that improve the flexural strength of the grouting medium with increased water resistance & minimal shrinkage. Tile Tak Tile Grout can be used to grout wall & floor tiles up to a maximum grout joint width of 8mm. The tile grout may also be used for grouting tiles in intermittently wet conditions.

Features
· Can be used on wall & floor tiles
· Can be used to tile joints of up to 8mm in width
· Waterproof
MIXING INSTRUCTIONS
· Mix 5kg of Tile Grout to 1.7lt of water to a fine paste.

· The product must be mixed to a creamy lump free consistency.

· For high taffic conditions replace the water in the mix with Tile Bond.

· Once mixed use the product within 2hrs.

· Do not add any additional water if the grout thickens once mixed.

SURFACE PREPARATION
These recommendations are in accordance with the SABS standard SANS – The design & installation of ceramic tiles.

· The tile adhesive must be completely set before the grout joints are grouted.

· Ensure the grout joint are free of any excess tile adhesive and are sound & free of dust and other contaminants.

· Grout joints are to be lightly moistened but not saturated before applying the tile grout.

APPLICATION OF TILE GROUT
· Apply the tile grout liberally into the grout joints ensuring that the joints are completely filled. A grout squeegee can be used.

· Remove the excess tile grout off the face of the tile once the grout joint has been filled.

· Smoothen off the tile grout whilst the grout is still wet.

· Allow the tile grout to harden in the grout joint, before removing the excess tile grout from the tile face. A damp cloth may be used to clean the tiles.

· Once the tile grout has completely set (after 24hrs) polish the tu=ile surface with a soft dry cloth.

COVERAGE
The coverage of the tile grout used is dependent on the dimensions of the tile grout joint. The amount of tile grout required can be theoretically calculated as follows:
· Kg of Tile Grout/m² = 
(A+B) x C x D X1.7





(AxB)
· Where A:
Is the length of the tile
· Where B:
Is the width of the tile

· Where C:
Is the thickness of the tile

· Where D:
Is the average width of the tile joint in mm  

PACKAGING 
· Tile Tak Wall & Floor Grout is supplied in 5kg & 20kg paper packets. 

· Store product off the floor and out of direct sunlight.
PRECAUTIONS

The following precautions must be adhered to:
· Ensure that the above instructions are adhered to at all times and do not adulterate the product in any way as this could result in tile failure.

· Rubber gloves should be used when applying Tile Tak Wall & Floor Grout. In the event of skin or eye irritation, rinse the affected area under cold water. Consult a medical doctor if the irritation persists.
· Keep the product away and out of reach from children and pets.
· Use a respirator when handling the product.
· This guideline only serves as a basic manual for the surface preparation product selection and installation procedure for this type of application. Each installation needs to be assessed and the products used, and the procedures followed should be in accordance with the SABS Code for the design and installation of ceramic tiles SABS 10107:2011

Tile Tak (Pty) Limited
22 Downie Crescent
Queensmead Industrial Area

Durban 4093
Telephone:
082 906 2365/083 661 6508 


E-Mail robb@tiletak.co.za
The information submitted on this data sheet is deemed correct. Tile Tak does not guarantee its accuracy but recommend that the user implements its own tests to determine suitability for the intended use. Tile Tak assumes no liability during all testing and use of this product. Tile Tak will replace any of the product proved to be defective. Tile Tak will assume no liability for any loss or damage relating to the use of this product. All products sold without any warranty 

